**APPLICATIONS**

• For ﬁlling and repairing small cracks and holes, such as drill holes and nails

• Excellent adhesion to plasterboard, wood, brick, concrete, ﬁber cement, drywall, plaster and render

• Not for use on metal, plastic, PVC and damp surfaces

• Suitable for interior & exterior use

**PRODUCT PROPERTIES**

• Ready to use

• Rapid dry: sand and paint after 15 minutes (5 mm layer at 20°C) with all types of paint

• Easy to sand

• Will not shrink

• Accepts nails and screws

• Maximum layer thickness: 5 mm

• Must be painted over when used outside (minimum 2 coats)

• Colour: White

**INSTRUCTIONS FOR USE**

• Substrate must be clean, dry, dust and grease free.

• Remove all loose materials.

• Mix the product well before use.

• Press fi­ller into crack with a fi­lling knife, smoothing off with a wet ­filling knife.

• For deeper repairs, build up in layers of 5 mm, letting the product dry in between layers.

• Remove any excess fi­ller and leave to dry.

• Once dry sand lightly if required.

• Clean tools and hands with warm water immediately after use.

• Do not store or use below 5°C.

**PACK SIZES**

330 g and 1 kg