| Description |  |
| --- | --- |
| Sikkens Autoclear Expert HS is two component clearcoat system provides excellent flow, gloss and smooth finish. It is easy to apply and suitable for all types of repairs, in most application conditions. |  |
| P Series Hardeners / Plus Reducers |  |
|  | 100 Autoclear Expert HS 50 P Hardeners - P25 / P35 5-10 Plus Reducer (Fast/Medium/Slow/Extra Slow) OR Xpress Dry Reducer |
|  | Use Sikkens measuring stick 3 Purple |
|  | Spray gun set-up: Application pressure: 1.3-1.4mm 1.7-2.0 bar at the air inlet HVLP max 0.6-0.7 bar at the air cap |
|  | 2 x 1 coat First apply a medium closed coat, next apply a full coat after indicated flash off time |
|  | Between coats Before curing 3-5 minutes at 25°C 10-15 minutes at 25°C Reducer selection according temperature Flash-off time depending on oven type |
|  | Product selection 25°C 60°C P25 / Xpress Dry Reducer 70 minutes 15 minutes P35 / Xpress Dry Reducer 80 minutes 25 minutes P25 / Plus Reducer Medium 180 minutes 33 minutes P35 / Plus Reducer Slow 210 minutes 40 minutes |
|  | Use suitable respiratory protection Akzo Nobel Car Refinishes recommends the use of a fresh air supply respirator. |
| Read complete TDS for detailed product information |  |

| Description |  |
| --- | --- |
| Sikkens Autoclear Expert HS is two component clearcoat system provides excellent flow, gloss and smooth finish. It is easy to apply and suitable for all types of repairs, in most application conditions. |  |
| ECO Hardeners and Reducers |  |
|  | 100 Autoclear Expert HS 50 ECO Hardeners - P25 / P35 10-15 ECO Reducers – Fast / Medium / Slow OR Xpress Dry Reducer |
|  | Use Sikkens measuring stick 3 Purple |
|  | Spray gun set-up: Application pressure: 1.3-1.4mm 1.7-2.0 bar at the air inlet HVLP max 0.6-0.7 bar at the air cap |
|  | 2 x 1 coat First apply a medium closed coat, next apply a full coat after indicated flash off time |
|  | Between coats Before curing 3-5 minutes at 25°C 10-15 minutes at 25°C Reducer selection according temperature Flash-off time depending on oven type |
|  | Product selection 25°C 60°C ECO P25 / Xpress Dry 55 minutes 11 minutes ECO P35 / Xpress Dry 70 minutes 18 minutes ECO P25 / Eco Reducer Med 120 minutes 25 minutes ECO P35 / Eco Reducer Slow 150 minutes 33 minutes |
|  | Use suitable respiratory protection Akzo Nobel Car Refinishes recommends the use of a fresh air supply respirator. |
| Read complete TDS for detailed product information |  |

Description

Sikkens Autoclear Expert HS is two component clearcoat system provides excellent flow, gloss and smooth finish. It is easy to apply and suitable for all types of repairs, in most application conditions.

Product and additives

Autoclear Expert HS Hardener P25 Hardener; spot and panel repairs at 15°C-25°C, larger areas 15°C- 20°C P35 Hardener; spot and panel repairs at 25°C-40°C, larger areas 20°C- 40°C ECO P25 Hardener; spot and panel repairs at 15°C-25°C, larger areas 15°C- 20°C ECO P35 Hardener; spot and panel repairs at 25°C-40°C, larger areas 20°C- 40°C Plus Plus Reducer Fast; spot and panel repairs at 15°C-20°C Reducers Plus Reducer Medium; spot and panel repairs and large areas at 15°C- 40°C Plus Reducer Slow; larger areas and complete paint jobs at 15°C- 40°C Plus Reducer Extra Slow; hot temperatures at 25°C - 40°C ECO Plus Reducer Fast; spot and panel repairs at 15°C-20°C ECO Plus Reducer Medium; spot and panel repairs, and large areas at 15°C- 40°C ECO Plus Reducer Slow; larger areas and complete paint jobs at 15°C- 40°C Xpress Dry Xpress Dry Reducer; spot and panel repairs at 15°C-25°C. Reducer Additives Elast-O-Actif __________________________________________________________________________________________ Mixing chart *Suggested hardener and reducer combinations, for best performance P25 Medium / Slow P25 Fast / Medium P25 Fast / Medium P25 Slow 15°C-20°C Medium / Slow P35 P25 Medium / Slow P25 Slow 20°C-25°C P35 Medium P35 Slow 25°C-30°C > 30°C Medium / Slow P35 Slow P35 Slow / Extra Slow P35 Slow / Extra Slow P35 Extra Slow P35 Slow P35 P35 Flash-off times are dependent on ambient temperature, air flow & job size Slow / Extra Slow

Basic raw materials

Basic Clear: Acrylic and polyester resins P Hardener: Poly-isocyanate resins Plus Reducers – A blend of organic solvents Xpress Dry Reducer: A blend of organic solvents, additives, and catalysts

Suitable substrates

Autobase Plus; after a minimum flash off time of 15 minutes at 25°C Autowave 2.0: until completely matt and dry

| Mixing with P Series Hardeners / Plus Reducers |  |
| --- | --- |
|  | Standard systems; Accelerated system. 100 Autoclear Expert HS; 100 Autoclear Expert HS. 50 P Hardeners; 50 P Hardeners. 5-10 Plus Reducers; 5-10 Xpress Dry Reducer. Use measuring stick No. 3 – Purple |
| Mixing with ECO Hardeners / Reducers |  |
|  | Standard systems; Accelerated system. 100 Autoclear Expert HS; 100 Autoclear Expert HS. 50 ECO Hardeners; 50 ECO Hardener. 10-15 ECO Reducers.; 10-15 Xpress Dry Reducer. Use measuring stick No. 3 – Purple |
| Viscosity |  |
|  | 14-17 seconds – DIN Cup 4 at 25°C. |
| Spray gun set-up / application pressure |  |
|  | Spray gun Fluid tip – set-up Application pressure Gravity feed 1.3-1.4 mm 1.7-2.0 bar at the spray gun air inlet HVLP max 0.6-0.7 bar at the air cap |
| Further recommendations for warmer climates greater than 30ºC |  |
| Based on test results when using Expert HS in warmer climates it is recommended to: - Choose a suitable Hardener / Reducer combination depending on ambient temperature & job size as suggested on mixing chart. - Only use 5% Plus Reducer - (1.4) fluid tip spray gun set-up |  |
| Application process & blending |  |
|  | Apply a medium closed coat, allowing for a 5-7 minutes flash-off time at 25°C. Next, apply a full coat, allowing for a 10-15 minutes flash-off time at 25°C before baking. Flash-off between coats; in case of application to larger areas, flash off between coats is minimal. Recoatable with itself after full drying cycle, sanding becomes necessary after 24 hours For blending (spot repair and panel blends), see TDS S8.01.01. When sanding and heavy polishing is required, a third coat may be applied after the stated flash-off times at 25°C. |
| Pot-life |  |
| P25 Hardener 2.5 hours at 25°C P35 Hardener >3 hours at 25°C P25 Hardener with Xpress Dry Reducer 1.5 hours at 25°C ECO P25 Hardener 1.5 hours at 25°C ECO P35 Hardener 2 hours at 25°C ECO P25 Hardener with Xpress Dry Reducer 1 hour at 25°C ECO P35 Hardener with Xpress Dry Reducer 1.5 hours at 25°C |  |

|  | Drying times |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Allow for a minimum of 10 minutes flash off time at 20°C - 30°C before moving the car into a pre-heated drying oven (booth) at 60°C. All drying times relate to standard application and object temperature. Consider the time required for the spray booth to reach an acceptable air temperature to enable the heat transfer of 60°C to the object. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  | P25 / Xpress Dry Reducer | P25 / Plus Reducer Med |  | P25 / Plus Reducer Slow |  |  |  | P35 /Plus Reducer Med |  |  | P35 /Plus Reducer Slow |  |  |  |
| 15°C |  | Dust dry |  | 18 minutes | 40 minutes |  | 45 minutes |  |  |  | 47 minutes |  |  | 50 minutes |  |  |  |
|  |  | Dry to handle* |  | 95 minutes | 360 minutes |  | 380 minutes |  |  |  | 400 minutes |  |  | 420 minutes |  |  |  |
| 25°C |  | Dust dry |  | 15 minutes | 25 minutes |  | 27 minutes |  |  |  | 30 minutes |  |  | 35 minutes |  |  |  |
|  |  | Dry to handle* |  | 70 minutes | 180 minutes |  | 200 minutes |  |  |  | 205 minutes |  |  | 210 minutes |  |  |  |
| 35°C |  | Dust dry |  | 12 minutes | 23 minutes |  | 25 minutes |  |  |  | 28 minutes |  |  | 30 minutes |  |  |  |
|  |  | Dry to handle* |  | 45 minutes | 70 minutes |  | 85 minutes |  |  |  | 90 minutes |  |  | 100 minutes |  |  |  |
| 60°C |  | Dust dry |  | 5 minutes | 15 minutes |  | 20 minutes |  |  |  | 22 minutes |  |  | 25 minutes |  |  |  |
|  |  | Dry to handle* |  | 15 minutes | 33 minutes |  | 35 minutes |  |  |  | 38 minutes |  |  | 40 minutes |  |  |  |
|  |  |  |  | ECO P25 / Xpress Dry Reducer | ECO P25 / ECO Med Reducer |  | ECO P25 / ECO Slow Reducer |  |  |  | ECO P35 / ECO Med Reducer |  |  | ECO P35 / ECO Slow Reducer |  |  |  |
| 15°C |  | Dust dry |  | 16 minutes | 25 minutes |  | 40 minutes |  |  |  | 43 minutes |  |  | 45 minutes |  |  |  |
|  |  | Dry to handle* |  | 90 minutes | 200 minutes |  | 210 minutes |  |  |  | 240 minutes |  |  | 300 minutes |  |  |  |
| 25°C |  | Dust dry |  | 14 minutes | 22 minutes |  | 26 minutes |  |  |  | 28 minutes |  |  | 33 minutes |  |  |  |
|  |  | Dry to handle* |  | 55 minutes | 120 minutes |  | 130 minutes |  |  |  | 135 minutes |  |  | 150 minutes |  |  |  |
| 35°C |  | Dust dry |  | 13 minutes | 20 minutes |  | 22 minutes |  |  |  | 25 minutes |  |  | 28 minutes |  |  |  |
|  |  | Dry to handle* |  | 40 minutes | 60 minutes |  | 65 minutes |  |  |  | 70 minutes |  |  | 75 minutes |  |  |  |
| 60°C |  | Dust dry |  | 4 minutes | 15 minutes |  | 17 minutes |  |  |  | 18 minutes |  |  | 20 minutes |  |  |  |
|  |  | Dry to handle* |  | 11 minutes | 25 minutes |  | 27 minutes |  |  |  | 30 minutes |  |  | 33 minutes |  |  |  |
|  |  |  | *Dry to handle; Following the drying cycle at 60°C object temperature, allow the Autoclear Expert HS to cool down fully to ambient temperature. Dry to handle after approximately 10 minutes. Allow 5 minutes flash off prior to infra-red curing The panel must not reach a temperature above 100°C while curing. For additional infra-red drying information; see TDS S9.01.01 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Polishability |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Dust and minor imperfections can be polished out after the stated air-dry times have been reached, or after a full bake at 60°C object temperature, followed by a cool down of the object to ambient temperature. Carefully sand out dust particles and restore the surface according polishing recommendations. Ready to polish approximately 30 minutes after cool down to ambient temperature. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Theoretical coverage |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | By using the recommended application, the theoretical material usage is ± 7 m²/liter RTS mixture. The theoretical material usage at 1μm dry film thickness is: 376 - 401 m²/liter The practical material usage depends on many factors i.e. shape of the object, roughness of the surface, application techniques, pressure and application circumstances. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Film Thickness |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | By using the recommended application: 50-60µm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Cleaning of equipment |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Sikkens Solvents or solvent borne Gun cleaners |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | VOC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | The VOC content of this product in ready to use form is 506 - 578 g/liter RTS mixture. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Product storage |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Product shelf-life is determined when products are stored unopened at 20°C. Avoid extreme temperature fluctuation. Product shelf life data see TDS S9.01.02 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Akzo Nobel Car Refinishes (Singapore) Pte Ltd

Address: 3 Changi Business Park Vista, #06-01 Akzo Nobel House, Singapore 486051

Tel: +65 6635 5262

FOR PROFESSIONAL USE WITH SUITABLE HS&E EQUIPMENT IMPORTANT NOTE The information in this data sheet is not intended to be exhaustive and is based on the present state of our knowledge and on current laws: any person using the product for any purpose other than that specifically recommended in the technical data sheet without first obtaining written confirmation from us as to the suitability of the product for the intended purpose does so at his own risk. It is always the responsibility of the user to take all necessary steps to fulfill the demands set out in the local rules and legislation. Always read the Material Data Sheet and the Technical Data Sheet for this product if available. All advice we give or any statement made about the product by us (whether in this data sheet or otherwise) is correct to the best of our knowledge but we have no control over the quality or the condition of the substrate or the many factors affecting the use and application of the product. Therefore, unless we specifically agree in writing otherwise, we do not accept any liability whatsoever for the performance of the product or for any loss or damage arising out of the use of the product. All products supplied and technical advices given are subject to our standard terms and conditions of sale. You should request a copy of this document and review it carefully. The information contained in this data sheet is subject to modification from time to time in the light of experience and our policy of continuous development. It is the user's responsibility to verify that this data sheet is current prior to using the product. Brand names mentioned in this data sheet are trademarks of or are licensed to Akzo Nobel. Head Office AkzoNobel Car Refinishes B.V., PO Box 3 2170 BA Sassenheim, The Netherlands. www.sikkenscr.com